MATERIAL DATA SHEET

PRODUCT:		26 - 140

Other Names		HR 140, RI26

PRODUCT TYPE:

Insulating Bricks and Slabs.

DESCRIPTION

Low Iron content, Fired Kaolinite.

Classification ISO 2245:  140	ASTM C155:  26

Maximum Classified Temperature:  1400°C.

Brick marking : 26-140.

CHEMICAL ANALYSIS:

XRF

Al 2O3		%	40.0

SiO2		%	54.0

Fe2O3		%	  1.2

TiO2		%	  1.3

CaO + MgO		%	  0.6

NaO + K2O		%	  2.6

PHYSICAL PROPERTIES:

Bulk Density		g/cm3	 0.87

Cold Crushing Strength		MPa	 4.7

Permanent Linear Change 12 hours at 1400°C	%	-0.6

Thermal Conductivity

(through 114mm dimension)	200°C	W/mK	0.28

400°C	W/mK	0.31

600°C	W/mK	0.34

800°C	W/mK	0.36

1000°C	W/mK	0.39

1200°C	W/mK	0.44

Reversible Thermal Expansion 20-1000°C	%	0.5

Pyroscopic Cone Equivalent		°C	1730

ADDITIONAL INFORMATION:

Recommended Mortar

Heat Set	C 1500 S or C 1500 H	(S = Dry , H = Ready to use)

Airset	RL 40 S or RL 40 H	(S = Dry , H = Ready to use)

The technical data in this publication is given for guidance only and is compiled from quality control results from normal production methods and is subject to normal process and raw material variations.Whilst every care is taken in the preparation of these figures , they are therefore approximate.Such data does not constitute a specification.

Chemical analysis is determined by XRF or Atomic Absorption on an ignited basis, Physical Properties are determined by BS1902, PRE or ISO standards.

www.swpuk.com